## Slide 1: ESC Introduction
Outline :
ESC 概論 ……… 鴻文。
深層 ESC ………. 建泓科技/ 研發經理 克民。
工商時間 ………. 建泓科技/ 羿凱。

## Slide 2: ESC 原理
ESC (Electrostatic Chuck) 靜電吸盤。
靜電吸盤 (ESC) 是一種特殊類型的夾具，用於通過靜電吸力通過電力壓住或拾取物體。
每一種物質都帶有內在的正電荷和負電荷。
當物體放置在 ESC 上並向其內部電極施加雙極電壓時，會產生定向電場，正電荷和負電荷會在材料內漂移，以匹配吸盤內部電極的極性。
ESC 和材料之間的這種吸引力就是所謂的靜電力，是我們靜電盤背後的基本機制。

## Slide 3: ESC 使用
晶圓製造過程中，當晶圓進入製程腔體後，需要將晶圓固定在腔體內的載具上以開始製程。
但一般機械式晶圓固定座(Mechanical Chuck)有邊緣損失及晶圓表面形變的問題。
適用 …大氣/真空下。
真空式晶圓固定座(Vacuum Chuck)，又有在真空式腔體內無法有效確實吸附固定晶圓之問題。
適用 … 大氣下。
靜電式晶圓座(Electrostatic Chuck , ESC)來當作晶圓箝制在製程腔體內的載具。
適用 … 大氣/真空下。
ESC
機械式固定座
Vacuum chuck
Vacuum pipe

## Slide 4: 傳統 Clamp Ring (機械式)
石英…圓形
陶瓷…圓形(平邊)
Vespel…Finger
陶瓷…Finger

## Slide 5: 傳統 Clamp Ring (機械式)
Process 需求 : Backside Helium …. Cooling wafer
Clamp ring 功用 ….. Fix wafer !
缺點 : Wafer 翹曲 ..均勻度不佳 !
破片風險高 ! Wafer edge 良率損失2~5 % 。
PEDSTAL
Clamp Ring
Wafer
Backside Helium (Servo 6 – 14 Torr)
Plasma (Pressure ~ < 0.5 Torr
Yield map :
Wafer edge 良率損失

## Slide 6: ESC
ESC (Electric Static Chuck)… 靜電吸盤。
優點 … 沒翹曲問題、均勻度佳、破片低、良率 (提升2 ~ 5% ) …. 可獲得改善。
ESC
Wafer
Backside Helium (Servo 6 – 14 Torr)
Plasma (Pressure ~ < 0.5 Torr

## Slide 7: ESC 種類(極性)
單極
雙極
ESC 的實際應用分為單極性和雙極性。

## Slide 8: ESC 種類(電介質)
以介電層材質為兩類。即庫侖類和JR(Johnsen-Rahbek )
吸盤與晶片接觸的表面有一層介電質。以前的吸盤用的介電質多為有機材料或陽極氧化層，現在已普遍採用陶瓷。純..介電質做成的吸盤為庫侖類，參雜…介電質做成的吸盤為迥斯熱背類(JR)。
介電質常見種類 … Al2O3 (陶瓷)
Anodizing (陽極氧化層)
Polyimide (聚醯亞胺 )
Al2O3
Anodizing
Polyimide

## Slide 9: 介電質
介電質是一種可被電極化的絕緣體。假設將介電質置入外電場，則束縛於其原子或分子的束縛電荷不會流過介電質，只會從原本位置移動微小距離，即正電荷朝著電場方向稍微遷移，而負電荷朝著反方向稍微遷移。

## Slide 10: 庫倫力
庫侖式靜電吸盤與晶片接觸的表面之介電層為高阻抗陶瓷材料。陶瓷層中有夾一層導電電極層，當電極被接通到高壓直流電源後，介電質的表面會產生極化電荷，分佈在晶片背面的電荷與分佈在吸盤上面的電荷極性相反，晶片即會被吸盤吸住。
介電層

## Slide 11: JR 力
當靜電吸盤使用的介電層材料為半導體材料時，稱為Johnsen-Rahbek 靜電吸盤(JR ESC)。其介電質表面不僅有極化電荷，還有很大部分自由電荷，這是因為JR吸盤的介電質有一定導電性。一般來說，JR吸盤的吸力比庫侖類的大。在對晶片溫度控制要求很高的蝕刻機中，越來越多採用JR靜電吸盤。
介電層

## Slide 12: ESC 應用… 新唐
(S200)離子植入機應用
Y11 以前是機械式載具，後續改為ESC。
需求 : Wafer plateform 需轉動與上下作動…0度/7度/30度不等 !
介電材質 : 六個陶瓷材質所做成的，做成三對扇型的形狀。
ESC Power : 這上面加上DC 雙極性矩形波電壓。
相位差120度，每相電壓 +/- 1000V ，接至3組 platen 。
A+
A-
B+
C+
B-
C-
wafer
Plateform
Beam way
機械式載具
ESC

## Slide 13: ESC 應用… 新唐
S500 蝕刻機應用
  Lam PE etcher
  EB etcher
  Lam ME etcher
  Oxide etcher
  Si etcher
ESC force
  庫倫力
  JR 力
極性
  單極/雙極
介電質
  陽極氧化層
  陶瓷
  Polyimide
ESC power
  700V
  1300 V
  5000 V
TEL
Lam 4520
Lam 4720
P5000
Trench
Lam 9500

## Slide 14: ESC 結構
正
背
背

## Slide 15: ESC 應用 … 新唐
Module | 型號/廠牌 | PROCESS | ESC Power | Force | Polar | Dielectrics | Film thickness | Roughness Ra(um) | Voltage range | On line (USE) | Maintenance
S200 | E500/VARIAN | IMPLANT | 直流方波三相1000V (120度) | Coulomb | 2 | Ceramic | 250um | 0.1~0.5 | >1000V | 4 | New/Refurbish
S500 | 9400/LAM | POLY ETCH | 直流 +/-350V | JR | 2 | Anodized | 45 ~ 60um | 0.4 ~ 0.8 | <700V | 7 | New/Refurbish/Clean
S500 | 4720/LAM | ETCH BACK | 直流 +/-350V | JR | 2 | Anodized | 45 ~60um | 0.4 ~ 0.8 | <700V | 6 | New/Refurbish/Clean
S500 | 9600/LAM | METAL ETCH | 直流 +/-350V | JR | 2 | Anodized | 45 ~ 60um | 0.4 ~ 0.8 | <700V | 4 | New/Refurbish/Clean
S500 | 4520/LAM | OXIDE ETCH | 直流 +/-350V | JR | 2 | Ceramic | 400um | 0.1~0.5 | <700V | 3 | New/Clean
S500 | 9500/LAM | OXIDE ETCH | 直流 +/-350V | JR | 2 | Anodized | 45~60um, | 0.4 ~ 0.8 | <700V | 3 | New/Clean
S500 | P5000/AMAT | OXIDE ETCH | 直流 1300 V | Coulomb | 1 | Polymide | 45 ~ 60um | <0.1 | >1000V | 10 | New/2nd
S500 | 65DD/TEL | Cotact | 直流 1500 V | Coulomb | 1 | Polymide | 45 ~ 60um | <0.1 | >1000V | 6 | New/2nd
S500 | C2L/STPS | Si ETCH | 直流 5000V | Coulomb | 1 | Ceramic | 1000um | 0.3 | >1000V | 1 | New
ESC 使用Type list :
依 ESC Power 、Force、Polar 、Dielectrics 共可分為 7 種 。

## Slide 16: 深層認識ESC
+
+
+
+
+
+
+
+
+
+
Electrode
Dielectrics
Wafer
+
+
+
+
+
+
+
+
+
+
+
+
y
V
d
‐
‐
‐
‐
‐
‐
‐
‐
‐
‐
ε
ε0
Plasma
Chucking force ?
庫倫力 / JR 力
單極/雙極
ESC power (電壓大小)
介電質 … 材質 / 膜厚 / 粗糙度 / …
功能檢驗… Helium / Flatness …
各種異常問題解析 ! ( Helium Leak 、吸不住 ! 黏片。 )
Base

## Slide 17
K-Max Technology
ESC 專家 : 克民 經理
深層認識ESC

## Slide 18
+
+
+
+
+
+
+
+
+
+
+
+
Electrode
Dielectrics
Wafer
+
+
+
+
+
+
+
+
+
+
+
+
y
V
d
Coulomb Force (庫侖力)
I= dQ/dt
Q=∫idt
e=(1/c)∫idt Q=c x e
E=CV2/2
=(ε0εSV2)/(2d)
Fc=∂E/ ∂d= ―(ε0εSV2)/(2d2)
Johnsen Rahbek Force (JR力)
I= dQ/dt
Q=∫idt
e=(1/c)∫idt Q=c x e
E=CV2/2
=(ε0εS’V2)/(2y)
Fj=∂E/ ∂d= ―(ε0εS’V2)/(2y2)
F = Fc + Fj
‐
‐
‐
‐
‐
‐
‐
‐
‐
‐
‐
ε
ε0
Plasma
Chucking Force
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 19
電容率
在電磁學裏，介電質響應外電場的施加而電極化的衡量，稱為電容率。在非真空中由於介電質被電極化，在物質內部的總電場會減小；電容率關係到介電質傳輸（或容許）電場的能力。電容率衡量電場怎樣影響介電質，怎樣被介電質影響。電容率又稱為「絕對電容率」，或稱為「介電常數」。
採用國際單位制，電容率的測量單位是法拉／公尺（Farad/meter，F/m）。真空的電容率，稱為真空電容率，或「真空介電常數」，標準值為 F/m 或 A2s4 kg-1m−3 。
ε0：真空電容率8.854187817×10-12 F/m
ε：相對電容率，又稱相對介電常數
真空：1
Helium gas：1.00000684
Argon gas：1.000127
Al2O3 ：9.8
AlN：8.8
Anodizing (aluminum oxide)：8
空氣：1.00054
水：88 (32°F)
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 20
Mono Polar
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
Open Circuit

## Slide 21
Bi Polar
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 22
ESC Structure
Lift Pin
Helium Hole
Chiller
Electrode
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
Thermal Couple
Electrode

## Slide 23
Function Data
Flatness
Roughness
Helium Pressure
Helium Leak Rate
Leak Current
Insulation
Di-electric Thickness
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 24
Flatness
Flatness
平面度不佳(形狀或是數值大)的狀況下，Wafer無法密合在ESC表面，因吸附力是接觸產生，若平面度不佳→吸附力不佳→Helium Leak大。
F = 最大值減最小值
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
CMM

## Slide 25
Roughness
粗糙度(Roughness)：加工的高頻因素所引起的高頻不規則表面，又稱為微
觀不平度，它是一種微觀何形狀誤差
Ra：中心線平均粗糙度
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
Roughness Meter

## Slide 26
Roughness
Rz：十點平均粗糙度
Ry (Rmax)：最大高度粗糙度
Rz、Rmax在DIN和ISO定稍微不同
Rz(DIN)：取五個樣品長度之平均全粗糙高度
Rz(ISO)：取評估長度中五個最高波峰、波谷間的平均距離。
故Rz(DIN)的數值會比較小；同理Rmax(DIN)也會比較小。Rmax = Ry
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 27
Roughness
表面粗糙度對ESC的功能性有什麼影響?
表面粗糙度值越大，在ESC表面的氦氣越容易流動，在外緣的氦氣越不容易保存在ESC與Wafer間，會有氦氣漏率過大的問題。
JR類型的ESC，表面粗糙度為靜電吸附產生的主要條件之一。粗糙度越大，ESC的吸附力越小；粗糙度越小，吸附力越大。
JR類型的雙極ESC，若各極於ESC表面的粗糙度差異太大，會造成de-chuck時的靜電殘留，而容易有Wafer Sticking的問題。
FJR = ∂E/ ∂y = ―(ε0εSV2) / (2y2)
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 28
Helium Function
Helium Pressure
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
維修前後的Helium Pressure比較
Helium Leak Rate
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
固定氦氣流量，確認固定時間內的氦氣壓力變化
固定壓力下，確認氦氣流量
Testing Chamber

## Slide 29
Insulation
Current Leakage
V = I R
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
To measure dielectric layer insulation
To measure electrode contact insulation
High Resistance Tester

## Slide 30
檢測設備
2.5D 量測儀
接觸式3D量測試儀
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 31
30
Roughness Meter
Thickness Tester
Insulation Meter
Leak Current Meter
檢測設備
Digital Microscope
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 32
Typical ESC Refurbishment
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 33
Chucking Force : Good He Leak Rate : Normal |  | 
Chucking Force : Decreased He Leak Rate : Increased |  | 
* Cause of Failure - Crack of Rib, Broken of Embossing, Erosion of Rib and Embossing, etc.. |  | 
AL Base
Ceramic puck
Embossing
Rib
Embossing
He
He
Embossing
Rib
He
He
Embossing
Rib
ESC Abnormal Issue
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 34
Before Refurbish | After Refurbish
Helium Leak Analysis
Helium leak cause by emboss consumed by plasma.
Outer Emboss recovered to flat condition after refurbish.
Outer Emboss
K-MAX
Helium Leakage
內
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 35
ESC Abnormal Issue
Helium flow
Wafer
Helium leakage through bonding layer
Refurbish Method：Re-bonding or Re-sealing
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 36
After Refurbish
500 X
2000 X
Before Refurbish
After Refurbish
Chucking Function Recovered
Surface Deposition Removed
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 37
Flatness and Roughness Recovered
After Refurbish
Step | Surface Flatness | 
Before Refurbish |  | 
Refurbished |  | 
Flatness = 12.6 μm
Flatness = 4.2 μm
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 38
生產流程
鋁材加工
-外型加工
-冷卻迴路
-氦氣迴路
表面處理
-陽極處理
-噴塗
陶瓷製造
-電極
貼合
-電極
-加熱器
加工
-平面度
-高度
-粗糙度
洗淨
測試
出貨
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 39
生產設備
鋁材加工
-外型加工
-冷卻迴路
-氦氣迴路
表面處理
-陽極處理
-噴塗
陶瓷製造
-電極
貼合
-電極
-加熱器
加工
-平面度
-高度
-粗糙度
洗淨
測試
出貨
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.

## Slide 40
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
K-MAX Technology CO,. Ltd.
ESC Function analysis / solution
K-MAX Technology Co., Ltd

## Slide 41
ESC Issue | K-max inspection | Reason | K-max Solution
B/H | He Pressure Test He Leak Rate test Flatness inspection Roughness check | 生成物/晶背金屬殘留堆積 ESC Surface flatness ESC glue layer damage Ceramic surface Roughness/ Emboss abnormal | Clean Refurbish
Sticking | He Pressure Test Sticking Test Roughness check | 生成物/晶背金屬殘留堆積 Emboss damage (Ra/高度) Leak Current High | Clean Refurbish
Leak Current | Current Leakage Test Microscope 耐電壓測試 | 1. 生成物/晶背金屬殘留堆積 2. Dielectric Layer厚度偏低 | Clean Refurbish
Chamber leak | Ceramic封閉測試 Chamber Leak Test | Edge Glue damage 測溫孔Glue damage | Sealing silicon glue
Etch Rate | He pressure test Flatness inspection Chiller check | 生成物/晶背金屬殘留堆積 Leak Current High Emboss Patten | Clean Refurbish
Arcing | Microscope check 耐電壓量測 | 生成物/晶背金屬殘留堆積 Ceramic Crack ESC Anodized damage 人為外力導致 | Clean Refurbish Re-plate
ESC Issue & Inspection & Solution

## Slide 42
K-Max Technology
Company Profile

## Slide 43
Worldwide Locations
K-MAX Technology Corporate
Established : 1965
Total Capital : USD5,000,000
Employees: 200 Staff

## Slide 44
Factory Location
  Total: 5 Floor,4,000 m2
  1F: Graphite Process Area
  2F: Lobby/ Metal Process /
  3D Measurement Area
  3F: Office/ Warehouse
  4F: ESC Production Line
  (Clean Room)
  5F: Restaurant

## Slide 45
Main Products
靜電系統研發製造
金屬石墨精密加工

## Slide 46
Manufacture Equipment
ESC Production Line

## Slide 47
Manufacture Equipment
Graphite Production Line

## Slide 48
Metal Production Line
Manufacture Equipment

## Slide 49: E-Chuck Material
Ceramic (Al2O3) ESC
Ceramic (AlN) ESC
Anodized ESC
Polyimide ESC

## Slide 50: E-Chuck Service
Brand New
Clean
Refurbish
Modify & Design

## Slide 51
DPS 8” / 12”
MXP
E-MAX 8” / 12”
MXP+
Super-E
Applications Etch
AMAT
Exelan
TCP
Exelan 2300
Versys 2300
PTX
LAM
DRM 8” / 12”
8500
85DP
SCCM 8” / 12”
SDRM
TEL
Producer

## Slide 52
In-House Repairs and Services
Typical Repair Steps
Disassemble
Clean
Bake Out
Re-Patterning
Anodizing
Bonding
Helium Leak Test
Function Test
Workshop Conditions
Custom Testing
Environmentally Controlled Workshop
All kinds ESC Refurbish
Class 1000 Clean Room
Class 1000
Class 1000

## Slide 53
1.
2.
3.
4.
5.
6.
7.
8.
9.
10.
11.
Inspection Tool
1.2D Measurement
2.Image Measuring Instrument
3.Force Measuring Instrument
4.Hardmess Measuring Instrument
5.3D Measurement
6.Roughness Meter
7.Thickness Tester
8.Digital Microscope
9.Leak Current Meter
10.Insulation Meter
11.Digital Microscope